# 项目周报

# Project Weekly Report

## 1. 本周工作内容

## 1. This Week’s Work

- 召开 7 月 15 日车间周会，梳理本周生产与质量问题。

- A shop-floor weekly meeting was held on 15 July to review production and quality issues.

- 6Cr13 批次 X-0702 完成热处理，硬度 56.2HRC，达标。

- Heat treatment completed for 6Cr13 batch X-0702, hardness 56.2HRC, within specification.

- 本周各工序生产与质量情况：

- Production and quality by process this week:

| 工序 | 数量（件） | 良率（%） | 备注 |
| --- | --- | --- | --- |
| 热处理 | 1200 | 97.7 | 崩口27件 |
| 磨削 | 1200 | 99.0 | 划伤37件 |
| 装配 | 1150 | 98.2 | — |

| Process | Qty (pcs) | Yield (%) | Notes |
| --- | --- | --- | --- |
| Heat treatment | 1200 | 97.7 | 27 chipped |
| Grinding | 1200 | 99.0 | 37 scratched |
| Assembly | 1150 | 98.2 | — |

## 2. 问题与风险

## 2. Issues and Risks

- 热处理工序本批崩口率 2.3%（炉号 0101~0148），高于内控 1.0%。主因：冷却槽风速偏低。措施：已通知设备组调整（责任方：设备组）。

- Chipping rate in heat treatment this batch: 2.3% (furnace no. 0101~0148), above the 1.0% internal limit. Cause: low air velocity in the quenching tank. Action: maintenance team notified to adjust (owner: maintenance team).

- 磨削开刃后手柄划伤 37 件。原因：防护贴失效。措施：已更换防护贴批次。

- 37 handles scratched after grinding/edge-setting. Cause: protective film failure. Action: replaced with a new batch of protective film.

- 客户 A 将于 8 月 12 日验厂到访，需提前准备食品接触材料检测报告；报告准备进度与责任人：【待补充：纪要未说明】。

- Customer A’s factory audit is scheduled for 12 August; food-contact material test reports must be prepared in advance; preparation progress and owner: [To be supplemented: not stated in the minutes].

## 3. 下周计划

## 3. Plan for Next Week

- 下周三前完成新刃型试模。

- Complete the new blade-type trial mould before next Wednesday.

- 李工负责备件清单，8 月底前提交。

- Spare-parts list (owner: Engineer Li) to be submitted before the end of August.

## 附

## Appendix

- B 中无未归入上述部分的孤儿内容；本部分按模板保留。

- No orphan content beyond the sections above; this section is kept per the template.